| 27 Upper Gordon Road Camberley Surrey GU15 2HJ | Chris Orkney HISTORIC BRICK MASON Shepperton cjo.hbm@gmail.com |
| --- | --- |
| Materials |
| Bricks : https://www.imperialhandmadebricks.co.uk/products/camberley-blend/ (samples acquired) Size: Imperial Lime mortars: All aggregates are to be washed NHL2 (St Astier) will act as the binder Laying Mortar : Ratio 2.5 parts Aggregate 1 part NHL2 All aggregates are to be washed NHL2 (St Astier) will act as the binder Pointing Mortars : Ratio 2.5 parts Aggregate 1 part NHL 2 Pigmentation as required |