Material Schedule

|  |  |
| --- | --- |
| From: | **Jack Bayliss LRTPI** |
| CC: | **Peter Leamy** |
| Date: | **8th February 2022** |
| Re: | **Material Schedule for Moat Barn House, Oldwich Lane East, Fen End, CV8 1NR** |

This Material Schedule considers the hardstanding materials for Moat Barn House, Oldwich Lane East, Fen End, CV8 1NR.

# brackendale cambrian sandstone - coventryBrackendale Sandstone – Marshalls <https://www.marshalls.co.uk/commercial/product/brackendale-sandstone>

**Finish:** Blasted finish.

**Material:** Sawn sandstone.

**Colour:** In shades ranging from pale grey/ beige to pale buff with red/ brown streaks and subdued banding.

**Nominal sizes:** [200 x 100 mm] [300 x 100 mm] [300 x 150 mm] [300 x 200 mm] [450 x 450 mm] [900 x 450 mm]

[900 x 600 mm] [900 x 600 mm].

**Slip Resistance:** Dry slip resistance (to BS 14231): 98. Wet slip resistance (to BS 14231): 78.

**Breaking load:** 27.5 MPa (Mean value to EN 12372: 2006 (Lev = 22.5 MPa)).

**Water absorption (maximum):** 1.2% (Mean value to EN 13755: 2008 (Hev =1.2%)).

# 10mm Gravel – Hanson <https://www.hanson-packedproducts.co.uk/en/products/base-aggregates/10mm-gravel>

10mm single sized gravel aggregate conforming to the requirements of BS EN12620: 2013.

**Typical moisture content:** 3%

**Particle size:** 4-10mm

**Shell content:** ≤ 10%

**Chloride content:** ≤ 0.01%

**Acid soluble sulphate:** ≤ 0.8%