| Customer |  |  | Madeira Drive | CIWS WO Number |  | 35294 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | MD ID Number |  | SP2 - TRIAL |  |  |
|  |  |  |  | Component Type |  | Spandrel Panel |  |  |
| Inspection Criteria |  |  |  | Results |  |  | Notes |  |
|  |  | Check tag attached to component |  |  |  |  |  |  |
| 1 |  | MPI |  | Yes – identify findings below |  |  | Insert Date of Inspection: 18/05/23 |  |
| 2 |  | Measurements taken |  | Yes– insert measurements as shown. |  |  | A = 2520mm B = 2305mm |  |
| 3 |  | Identify any cracks mark on casting with yellow pen and mark on drawing |  |  |  |  | Cracks found Major cracks at right angle top lefthand corner |  |
| 4 |  | Check for pitting corrosion >5mm in depth and >5mm in diameter mark on casting with yellow pen and mark on drawing |  |  |  |  | Small amount of pitting |  |
| 5 |  | Check for decorative repair mark with yellow pen on casting and mark on drawing |  |  |  |  | Piece broken off |  |
| 6 |  | Identify any damaged bolt holes mark on casting and on drawing. Detail any other defective area to include cracks propagating to surface lamination. Ensure screw bolts are removed and retained. |  |  |  |  | Thread Diameters : Screw bolt stuck once pre-heated for repairs bolt expected to become loose |  |
| 7 |  | Photo taken once inspection complete, and all areas marked take multiple photos of defect areas |  | Yes Min 2 Max 4 |  |  |  |  |
| - Pre-Repair Photographs: |  |  |  |  |  |  |
| - Photo 1: |  |  |  | - Photo 2: |  |  |
| - Photo 3: |  |  |  | - Photo 4: |  |  |
| - Post Repair Photographs: |  |  |  |  |  |  |
| - MPI Date: - Weld Date: - Welder: - DPI Date: |  |  |  |  |  |  |
| - Photo 1: |  |  |  | - Photo 2: |  |  |
| - Photo 3: |  |  |  | - Photo 4: |  |  |